## Slide 13
Updated energy profile for chlorobenzene on Cu(111)

## Slide 14
Updated energy profile for bromobenzene on Cu(111)

## Slide 15
Updated energy profile for iodobenzene on Cu(111)

## Slide 16
Updated energy profile for iodobenzene on Cu(111)
+0.88 eV

## Slide 17
100K, 0.001 molecule/nm^-2
All following free E are bromobenzene on Cu(111)

## Slide 18
100K, 0.01 molecule/nm^-2

## Slide 19
100K, 0.1 molecule/nm^-2

## Slide 20
200K, 0.1 molecule/nm^-2

## Slide 21
300K, 0.1 molecule/nm^-2

## Slide 22
Updated energy profile for bromobenzene on Cu(111)
-0.93 eV
-2.00 eV
+0.88 eV

## Slide 23
400K, 0.1 molecule/nm^-2

## Slide 24
500K, 0.1 molecule/nm^-2

## Slide 25
Updated energy profile for bromobenzene on Cu(111)

## Slide 26
Bromobenzene on Ag(111)
1.53
-0.62
-1.38
TS-ad
TS1
Ts-g
-0.33
TS-r2

## Slide 27
Bromobenzene on Au(111)
TS1
-0.41
TS-ad
1.73
Ts-g
-0.72
-0.45

## Slide 28
Bromobenzene on Ag(111)

## Slide 29
Bromobenzene on Au(111)

## Slide 30
Bromobenzene on adatom-Cu(111)