## Slide 1
Updated energy profile for bromobenzene on Cu(111)

## Slide 4
0.00
0.17
0.99
1.56
Notes: I did not realize that the DHAL-2 state need to be doubled from DHAL state. In this figure, I only count as DHAL state, so I corrected in next figure

## Slide 5
Freeze
(a)
0.06
0.90
1.29
0.44
0.89
1.39
(b)
Notes: CMC_state(relaxed) – CMC_surfaceonly(single_point) – CMC_state = $delta$ (zero-reference)

## Slide 6
Phenyl-assisted adatom extraction is difficult
C-C bond formation on adatoms is slow
Efficient adatom catalysis
Line of thermoneutral extraction

## Slide 7
Relaxation
Notes: Interaction1 = Ph-Metal-Ph – 2 * Ph(relaxed) – Metal * 1
Interaction2 = CMC(relaxed) – 2 * Ph(relaxed) – pure_surface(relaxed)
Energy = interaction1-inreaction2

## Slide 8
Bromobenzene on adatom-Cu(111) and Au(111), existing adatom
+1.76
-2.13
-2.62
-3.57
-1.79
-4.05
+1.56
+0.81
+0.07
-0.52
-0.32
-2.17
Notes: RZK: X-DIM-A state -> all three states are dark grey.

## Slide 9
0.00
-3.89
-4.38
-5.33
-3.55
-5.81
-0.75
-1.49
-2.08
-1.88
-3.73

## Slide 10
-3.90
-3.73
-2.35
-3.94
-3.57
-3.24
-1.24
-3.18
-3.02
-4.06
-1.78
Notes: X-CMC to X-DIM-A: two phenyl ring are very far in transition state, they arise to form a C—C bond on top of a copper, their pai interaction with copper surface is drastically decreased; CMC-DIM, two phenyl ring always stay close to surface and to each other, their pai-system are ready to built.
X-DIM-A: the biphenyl are not planar, it distort the pai-system and decrease its interaction with surface
X-CMC: red C—C 3.89, C—Cu 1.94 C—Sur 2.27
CMC C—C 3.10 C—Cu 2.05
X-CMC(Transition state): red line, two phenyl ring is very high on surface, almost parallel. C—C 2.53, C—Cu 1.89 C—Sur 3.42
CMC(Transition state): still tilt, interact with lifted copper C—C 2.28 C--Cu 2.02
X-DIM-A red C—C 1.50 C—Cu 2.17 C—Sur 3.58
DIM C—C 1.49 C—Cu 3.21

## Slide 12
0.00
-1.14
-0.25
-1.95
-3.90
-3.73
-3.24
-3.02
-3.57
-1.79
-4.06
-3.97
-2.25
+1.83
+1.76
+2.04
-5.73
-4.01
+0.07
Notes: Extraction: 1.78
Ideal surface: 0.

## Slide 13
0.00
-1.14
-0.25
-1.95
-3.90
-3.73
-3.24
-3.02
-3.57
-1.79
-4.06
-3.97
-2.25
+1.83
+1.76
+2.04
-5.73
-4.01
+0.07

## Slide 14
Ag(111)
0.00
-0.92
+0.28
-0.88
-1.76
-2.01
-1.39
-1.58
-1.87
-0.35
-3.13
-3.48
-2.12
+1.63
+1.56
+1.72
-4.78
-3.43
+0.07
Notes: Extraction: 1.52
Ideal surface: 0.62

## Slide 15
Au(111)
0.00
-1.06
+0.40
-0.37
-0.74
-0.88
-0.74
-0.52
-0.52
-0.32
-2.17
-2.04
-0.47
+1.62
+1.56
+1.72
-3.59
-2.03
+0.07
Notes: Extraction: 0.2
Ideal surface: 0.14

## Slide 16
Ag
Cu
Au

## Slide 17
CMC
DIM‡
DIM
X-CMC‡
X-CMC
X-DIM‡
X-DIM
X-DIM
X-DIM‡
X-CMC
X-CMC‡
DIM‡
DIM
X-CMC‡
X-CMC
X-DIM
X-DIM‡
X-CMC
X-CMC‡
CMC
X-DIM
X-DIM‡

## Slide 18
CMC
DIM‡
DIM
X-CMC‡
X-CMC
X-DIM‡
X-DIM
X-DIM‡
X-CMC
X-CMC‡
X-DIM
（a)

## Slide 19
CMC
DIM‡
DIM
X-CMC‡
X-CMC
X-DIM‡
X-DIM
X-DIM‡
X-CMC
X-CMC‡
X-DIM
CMC
DIM‡
DIM
CMC
DIM‡
DIM
X-DIM
X-DIM‡
X-CMC
X-CMC‡
X-DIM
X-DIM‡
X-CMC
Cu
Ag
Au

## Slide 20
CMC
DIM‡
DIM
X-CMC‡
X-CMC
X-DIM‡
X-DIM-A
X-DIM‡
X-CMC
X-CMC‡
X-DIM-A
CMC
DIM‡
DIM
CMC
DIM‡
DIM
X-DIM-A
X-DIM‡
X-CMC
X-CMC‡
X-DIM-A
X-DIM‡
X-CMC
Cu
Ag
Au
(a)

## Slide 21
CMC
DIM‡
DIM
X-CMC‡
X-CMC
X-DIM‡
X-DIM-A
X-DIM‡
X-CMC
X-CMC‡
X-DIM-A
CMC
DIM‡
DIM
CMC
DIM‡
DIM
X-DIM-A
X-DIM‡
X-CMC
X-CMC‡
X-DIM-A
X-DIM‡
X-CMC
Cu
Ag
Au
(a)

## Slide 22
C-Br break

## Slide 23
PHYS
DHAL‡
DHAL
C-Cl break

## Slide 24
PHYS
DHAL‡
DHAL
C-I break

## Slide 26
0.00
-1.14
-0.25
-1.95
-3.90
-3.73
-3.24
-5.73
-4.01
0.07
-1.14
-0.25
-1.95
-3.90
-3.73
0.00
-0.25
-1.95
-3.90
-3.73
0.00
-1.24
-3.18
-2.35
-3.94
-1.93
-4.11
-3.97
-2.25
+1.83
-1.24
-3.18
-1.14
-3.02
-3.57
-1.79
-4.06
-3.97
-2.25
+1.83
PHYS
DHAL‡
DHAL
DHAL-2
CMC
DIM‡
DIM
DSRB-D
DSRB-A
SURF
PHYS
DHAL‡
DHAL
DHAL-2
CMC
SURF
DHAL‡
DHAL
DHAL-2
CMC
PHYS
X-DHAL
X-DHAL-2
X-CMC‡
X-CMC
X-DIM‡
X-DIM-A
X-DIM-B
X-DSRB-D
X-DSRB-A
X-DHAL
X-DHAL-2
X-CMC
X-DIM‡
X-DIM-A
X-DIM-D
X-DSRB-M
X-DSRB-A
X-CMC‡
SURF
Red and Yellow should change the label !!!
Not emergent

## Slide 27
Notes: The last state now is the pure surface + dimer in gas + two bromine atom in gas (0.07eV, not 0.00 eV anu more)
This figure only counts translational partition in free energy calculation.

## Slide 28
Notes: This figure only counts both translational and rotational partition in free energy calculation

## Slide 29
Legend: Adatom extraction along
Legend: Adatom extraction along
Place this drawing in one of the surface figures: