## Slide 1
Updated energy profile for bromobenzene on Cu(111)

## Slide 2
Bromobenzene on adatom-Cu(111)
DHAL
PHYS
X-PHYS
X-DHAL-3
Notes: Lack of some states figures (in diagram)

## Slide 3
-3.90
-3.73
-2.35
-3.94
-3.45
-3.24
Notes: X-CMC to X-DIM-A: two phenyl ring are very far in transition state, they arise to form a C—C bond on top of a copper, their pai interaction with copper surface is drastically decreased; CMC-DIM, two phenyl ring always stay close to surface and to each other, their pai-system are ready to built.
X-DIM-A: the biphenyl are not planar, it distort the pai-system and decrease its interaction with surface
X-CMC: red C—C 3.89, C—Cu 1.94 C—Sur 2.27
Black C—C 3.10 C—Cu 2.05
X-CMC(Transition state): red line, two phenyl ring is very high on surface, almost parallel. C—C 2.53, C—Cu 1.89 C—Sur 3.42
Black line: still tilt, interact with lifted copper C—C 2.28 C--Cu 2.02
Final red C—C 1.50 C—Cu 2.17 C—Sur 3.58
Black C—C 1.49 C—Cu 3.21

## Slide 4
Ag(111)

## Slide 6
Notes: The last state now is the pure surface + dimer in gas + two bromine atom in gas (0.07eV, not 0.00 eV anu more)
This figure only counts translational partition in free energy calculation.

## Slide 7
Notes: This figure only counts both translational and rotational partition in free energy calculation