## Slide 1
Updated energy profile for bromobenzene on Cu(111)

## Slide 2
Bromobenzene on adatom-Cu(111)
DHAL
PHYS
X-PHYS
X-DHAL-3
Notes: Lack of some states figures (in diagram)

## Slide 3
-3.90
-3.73
-2.35
-3.94
-3.57
-3.24
-1.24
-3.18
-3.02
-4.06
-1.78
Notes: X-CMC to X-DIM-A: two phenyl ring are very far in transition state, they arise to form a C—C bond on top of a copper, their pai interaction with copper surface is drastically decreased; CMC-DIM, two phenyl ring always stay close to surface and to each other, their pai-system are ready to built.
X-DIM-A: the biphenyl are not planar, it distort the pai-system and decrease its interaction with surface
X-CMC: red C—C 3.89, C—Cu 1.94 C—Sur 2.27
CMC C—C 3.10 C—Cu 2.05
X-CMC(Transition state): red line, two phenyl ring is very high on surface, almost parallel. C—C 2.53, C—Cu 1.89 C—Sur 3.42
CMC(Transition state): still tilt, interact with lifted copper C—C 2.28 C--Cu 2.02
X-DIM-A red C—C 1.50 C—Cu 2.17 C—Sur 3.58
DIM C—C 1.49 C—Cu 3.21

## Slide 4
Ag(111)

## Slide 6
Chart: C--C distance (A)
| 3.1 | 2.96 | 2.72 | 2.2799999999999998 | 1.58 | 1.5 | 1.49 | 1.49
ideal-surface | -3.73 | -3.6693 | -3.4701 | -3.2405 | -4.7666 | -5.425 | -5.6648 | -5.7573
extraction-1 | -3.734 | -3.6547 | -3.4703 | -3.2032 | -2.8074 | -2.4156 | -2.3569 | -2.3991 | -2.6723 | -3.2203 | -3.5466 | -3.7713 | -3.9166 | -3.9383
extraction-2 | -3.9383 | -3.8908 | -3.6762 | -3.0933 | -2.4059 | -2.1234 | -1.9756 | -1.9328 | -2.4671 | -3.7305 | -4.0854 | -4.1109
Chart: Distance between center of mass (A)
| 4.9095861799999998 | 4.9372169399999999 | 4.86805705 | 4.6507564400000003 | 4.3775108200000004 | 4.3615144199999998 | 4.40222494 | 4.4156019000000004
ideal surface | -3.73 | -3.6693 | -3.4701 | -3.2405 | -4.7666 | -5.425 | -5.6648 | -5.7573
extraction-1 | -3.734 | -3.6547 | -3.4703 | -3.2032 | -2.8074 | -2.4156 | -2.3569 | -2.3991 | -2.6723 | -3.2203 | -3.5466 | -3.7713 | -3.9166 | -3.9383
extraction-2 | -3.9383 | -3.8908 | -3.6762 | -3.0933 | -2.4059 | -2.1234 | -1.9756 | -1.9328 | -2.4671 | -3.7305 | -4.0854 | -4.1109

## Slide 8
Notes: The last state now is the pure surface + dimer in gas + two bromine atom in gas (0.07eV, not 0.00 eV anu more)
This figure only counts translational partition in free energy calculation.

## Slide 9
Notes: This figure only counts both translational and rotational partition in free energy calculation